Homework  08 (for Conradt lectures):
Due date  for  both parts is Thursday, April 15, 2010

Part A:  From Lecture 21
Derive the enthalpy and entropy (T = 298 K) of a glass of composition (in wt. %)
65 SiO2, 15 Al2O3, 20 CaO.

Compare the result to the values of the isochemical (polycrystalline) equilibrium state.  
What is the Gibbs energy difference at 298 K?

With a value of Tg= 760 °C and Hfus= 475 kJ/kg as given, what estimate do you derive for Cp?  
What is the expected fragility slope?

Part B: (from lecture 22, slide 60)