Questions from Feller Parts 1, 2, and 3

1. What is the packing of the face centered cubic structure?

Answer: 0.74.

2. Find the crystal structure, including dimensions, of aluminum.  Using its packing fraction from this known structure and its atomic mass predict the density.  Compare with experiment.

Final Answer: 2.70 g/cc

3. Imagine a 0.7 cc of a lead silicate glass of density 7.5 g/cc.  What is its apparent weight in

a) water

b) diiodomethane

c) carbon tetrachloride

4. What temperature control of the fluid would it take to allow measurements with an error no more than 0.5 %.

5. Plot the densities of liquid mixtures of acetone and diiodomethane as a function of the mass ratio of diiodomethane to acetone assuming they are fully miscible.

6. Use http://www.ides.com/property_descriptions/ASTMD1505.asp to find out about the density gradient method.  Nothing need be turned in here.

7. R = x/(1-x)	Density (g/cc)

- 0·0		1·82

- 0·2		2·68

- 0·2		2·66

- 0·4		3·35

- 0·4		3·29

- 0·6		3·71

- 0·6		3·68

- 0·8		3·95

- 0·8		3·90

- 0·9		4·09

- 1·2		4·22

- 1·3		4·31

- 1·5		4·40

- 1·7		4·50

- 2·0		4·53

Use these data from the barium borates and the borate model to find the four basic borate volumes.  Note this model might not yield exactly the volumes given before.

8. Calculate the molar volumes of the barium borates given before.  You will need atomic masses.  Also, remember that the data are given in terms of R and there are R+1 moles of glassy materials.  You could also use x to do the calculation.

9. For the barium borate data provided earlier plot the volume per mol boron oxide as a function of R. How do you interpret the result?

10. 	a) Determine the packing fractions of the barium borate glass system.

b) Using the known density of BaO compare the packing fraction of the crystal to

the glasses.

c) Plot all results. How do the results compare to the alkali borates?

References for Density from the Coe Glass Group

“Packing as a Probe of Structure in Alkaline Earth Glass Systems” with M. Burgess, D.

McClarnon, M . Affatigato, and S. Feller, J. Non-Cryst. Solids 354 3491-3502 (2008).

“Density and Glass Transition Temperature Study of Low-Alkali Content Vanadate

Glasses,” submitted to Phys. Chem. Glasses with  J. Helmus, J. Lewis, C.P. O’Brien,

S. Shrestha,  M. Affatigato, and S. Feller (2006).

“A Solution Approach to High Alkali Content Borate Glasses,” Phys. Chem. Glasses:

Europ. J. of Glass Science and Tech. 47(4) 328-331 (2006) for the Proceedings of the

Fifth International Conference on Borate  Glasses, Crystals and Melts

(Trento, IT) (2005) with J. Banerjee, G. Ongie, J. Harder, T. Edwards, C. Larson,

S. Sutton, A. Moeller, A. Basu, M. Affatigato, S. Feller, M. Kodama.

“Differential Volume Changes in Trigonal and Tetrahedral Borate Units,” Phys. Chem

Glasses:Europ. J. of Glass Science and Tech. 47(4) 543-547 (2006) for the Proceedings

of  the Fifth International Conference on Borate  Glasses, Crystals and Melts (Trento, IT)

with G.J. Ongie, S.A.Feller, M. Affatigato, M. Kodama.

# “A General Study of Packing in Alkali Glass Systems,” with S. Giri, C. Gaebler, J. Helmus,

# M. Kodama, M. Affatigato, and S. Feller, J. Non-Cryst. Solids 347 (2004) 87-92.

“Glass Formation, Molar Volumes and Glass Transition Temperatures of Binary Vanadate

Glasses,” Phys. Chem. Glasses 44(1), 1-4 (2003), with A. Basu, J. Lewis, C.P. O’Brien,

H. Feller, S. Starns, J. Frueh, S. Feller, and M. Affatigato (2002).

“A Study of Packing in Alkali Borate Glasses,” Phys. Chem. Glasses 44(3), 230-233

(2003) as part of the Proceedings of the Fourth International Conference on Borate

Glasses,Crystals and Melts with E. Hemesath, S. Giri, S. Feller, and M. Affatigato

“The Physical Properties of Barium Borosilicate Glasses Related to Atomic Structure,”

Phys. Chem. Glasses 44(3) 207-211 (2003) as part of the Proceedings of the Fourth

International Conference on Borate Glasses, Crystals and Melts with A. Betzen,

B. Kudlacek, S.Kapoor, J. Berryman, N. Lower, H. Feller, M. Affatigato, and S. Feller.

“A Solution Approach to High-Potassium Content Borate Glasses,”  Phys.Chem

Glasses 44(3) (2003) 237-240 as part of the Proceedings of the Fourth International

Conference on  Borate Glasses,Crystals and Melts with A. Moeller, M. Olesiak, J. Gao,

S. Giri, M. Affatigato, and S. Feller.

“The Intermediate Range Order of Borate Glasses Related to Elastic Properties,”  Phys

Chem Glasses 44(2) (2003) 117-120  as part of the Proceedings of the Fourth

International Conference on Borate Glasses, Crystals and Melts with S. Feller,

M. Affatigato, S. Giri, A. Basu, and  M. Kodama.

“Density as a Probe of Oxide Glass Structure,”  Phys. Chem. Glasses  42(3) (2001)

pp. 240-246 with S. Feller, N. Lower, and M. Affatigato.

“Physical Properties of Alkaline-Earth Borate Glasses Prepared Over an Extended Range

of Metal Contents,” J. Non-Cryst. Solids 293-295 (2001) pp. 669-675, with N.P. Lower,

J.L. McRae, H.A. Feller, A.R. Betzen, S. Kapoor, M. Affatigato, and S.A. Feller

“Physical Properties of Alkali and Mixed Lithium-Cesium Vanadate Glasses Prepared Over

an Extended Range of Compositions,”  J. Non-Cryst. Solids 293-295 (2001) pp. 663-668,

with J.M. Lewis, C.P. O’Brien, M. Affatigato, and S.A. Feller.

“Study of the Physical Properties of Alkali Germanate Glasses Over Wide Ranges of

Composition,” J. Non-Cryst. Solids 272 (2000) pp. 57-66 with T.J. Kiczenski, C. Ma,

E. Hammarsten, D. Wilkerson, M. Affatigato, and S. Feller

“Physical Properties of Lithium Borovanadate Glasses Related to Atomic Arrangement,”

Proceedings of the Third International Conference on Borate Glasses, Crystals and Melts

in Phys. Chem. Glasses 41(6) (2000) 341-344 (Ed. A.C. Wright) with H. Feller,A.Betzen,

M. Affatigato, and S. Feller.

“Physical Properties of Sodium Borogermanate Glasses Compared with the Sodium

Borosilicate System,” Proceedings of the Third International Conference on Borate

Glasses, Crystals and Melts in Phys. Chem. Glasses 41(6) (2000) 365-368.  (Ed. A.C.

Wright), with C.Ma, T. Kiczenski, E. Hammarsten, J. Mcrae, M. Affatigato, and S.

Feller.

“Physical Properties of Barium Borate Glasses Determined over a Wide Range of

Compositions,” J. Non-Cryst. Solids 270, 215-222 (2000) with S. Kapoor, H.B. George,

A. Betzen, M. Affatigato, and S. Feller.

“Density and Molar Volume of Extremely Modified Alkali Silicate Glasses,”

Phys.Chem. Glasses 40(6), 339 (1999) with H. Doweidar, S. Feller, M. Affatigato,

B.Tischendorf, C. Ma, and E. Hammarsten.

“The Density of Alkali Silicate Glasses Over Wide Compositional Ranges,” Journal of

Non-Crystalline Solids 239, 197-202 (1998)  with B. Tischendorf, C. Ma, E.

Hammarsten, P.Venhuizen, M. Peters, M. Affatigato, and S. Feller.

“Physical Properties of Alkali Borosilicate Glasses,”  Proceedings of the Second

International Conference on Borate Glasses, Crystals and Melts (Ed. A.C. Wright,

S.A. Feller, A.C.Hannon) (Society of Glass Technology:Sheffield,UK) pp.246-253 (1997) with S. Feller, J. Kottke, J.Welter, S. Nijhawan, R. Boekenhauer, H. Zhang, D. Feil,

C. Paramswar, K. Budhwani, M.Affatigato, G.Bhasin, S. Bhowmik, J. MacKenzie,

M. Royle, S. Kambeyanda, P. Pandikuthira, and M.Sharma.

“A Comparison of the Densities of Lithium and Sodium Borate and Silicate Glasses with

Very High Alkali Contents,” Proceedings of the Second International Conference on

Borate Glasses, Crystals and Melts (Ed. A.C. Wright, S.A. Feller, A.C.Hannon) (Society

of Glass Technology:Sheffield,UK) pp.498-505 (1997) with P.Venhuizen, A.M.Peters,

F. Alamgir, K. Loh, R. Williams, and S. Feller.

“A Density Model for the Lithium, Sodium, and Potassium Borosilicate Glass Systems,”

Physics and Chemistry of Glasses, 36(4), 183-190 (1995) with K. Budhwani and S.

Feller.

“The Density of Lithium Silicate Glasses Over an Extended Range of Compositions,”

Physics and Chemistry of Glasses, 35(5), 212-215 (1994) with A.M. Peters,

F.M. Alamgir, S.W. Messer, S. Feller, and K.L. Loh.

“Physical Properties of Alkali Borosilicate Glasses Related to Atomic

Arrangements,” Proceedings of the International Symposium on Glass Science and

Technology (Athens, Greece), Oct 1993, as published in Chemika Chronika (New Series)

23 (2,3) 315-321 (1994)with S. Feller, R. Boekenhauer, H. Zhang, D. Bain, D. Feil,

C. Parameswar, K. Budhwani, S. Ghosh, S. Nijhawan, & J. MacKenzie.

“Densities and Structural Models Resulting from Extremely Modified Cesium and

Rubidium Borate Glasses,” Physics and Chemistry of Glasses, 34(4), 149-152 (1993)

with M. Royle, M. Sharma, S. Feller, J. MacKenzie and S. Nijhawan.

“The Density of Sodium Borosilicate Glasses Related to Atomic Arrangements,” Journal

of Non-Crystalline Solids, 119, 103-111 (1989) with D. Feil and S. Feller.

“The Density of Two Mixed Alkali Borate Glass Systems Related to Atomic 	Arrangements,” Journal of Non-Crystalline Solids, 109, 105-113 (1989) with B. Chong,

S. Choo, B. Teoh, E. Khaw, D. Feil, K.Chong, S. Feller, M. Affatigato, D. Bain, K.

Hazen, and K. Farooqui.

“Thermal Effects on Density of Alkali Borate Glasses” proceedings of the Second

International Conference on Effects of Modes of Formation on the Structure of Glass

Diffusion and Defect Data, 53-54 277-282 (1987) with H.C. Lim and S. Feller.

“The Density of Low Metal Content Rubidium, Cesium, Silver, and Thallium Borate

Glasses Related to Atomic Arrangements,” Journal of Non-Crystalline Solids, 94, 36-44

(1987) with H.C. Lim and S. Feller.

“The Density of Potassium Borate Glasses Related to Atomic Arrangements,” Journal of

Non-Crystalline Solids, 91 324-332 (1987) with H.P. Lim, A. Karki, S. Feller, J. Kasper,

and G. Sumcad.

“The Density of Sodium Borate Glasses Related to Atomic Arrangements,” Journal of

Non-Crystalline Solids, 92 11-19 (1987) with A. Karki, H.P. Lim, S. Feller, J. Stark,

C. Sanchez, and M. Shibata.

“The Density of Lithium Borate Glasses Related to Atomic Arrangements,” Journal of

Non-Crystalline Solids, 85 29-41 (1986) with M. Shibata, C. Sanchez, H. Patel, J. Stark,

S. Feller, G. Sumcad and J. Kasper