HOMEWORK: Passive Optical Properties of Glass:

- Use Ref 1 & 2 and other relevant articles you can find to explain in detail why femtosecond photo-writing works well in SiO2 but not so well in phosphate glass.

- From the attenuation curve on slide 15 of lecture 3, estimate how many amplifiers you would need to build a telecom network from LA to NY (4500km) at 1.55 microns vs 0.8 microns considering that amplification is required when the power fall to 10% of its initial value.

- Qualitatively, in which of the three following glasses do you expect a beam of light to propagate the slowest? Explain you choice.

A- 54 SiO2-5 PbO-19 B2O3-10 Na2O- 12 CaO

B- 34 SiO2-37 PbO-9 B2O3-5 Na2O- 10 CaO

C- 46 SiO2-24 PbO-12 B2O3-8 Na2O- 7 CaO

- The headlights of a car are reflected off a shop window normal to the glass surface. The headlight intensity is Io= 12 mW/cm2 and the reflected intensity off the surface of the window is I= 0.98 mW/cm2. What is the refractive index of the soda-lime-silicate glass window?

- Using Ref [1] (Fig 3, 5, 6), (a) calculate the absorption coefficient at 0.2 micron of type II silica assuming the measurements of Fig 3 were performed on a slab of thickness 1 cm and that it was annealed with a Tf of 1200C. (b) Estimate the change in Transmission when you raise the temperature from room T to 900C. Assume there is no scattering and the absorption coefficient is independent of temperature.

- Look up the bandgap of MCT (HgCdTe) in the literature (a good ref is Handbook of Infrared Detection Technologies By Mohamed Henini, M. Razeghi ) and explain why MCT is a good detector for the mid-IR and why it must be cooled with liquid N2.

Reference

[1]. R. Bruckner JOURNAL OF NON-CRYSTALLINE SOLIDS 5 (1970) 123-175

[2]. D.M. Krol, J.W. Chan, T.R. Huser, S.H. Risbud, J.S. Hayden, Proc.SPIE 5662 (2004) 30